**NEW PRODUCT SERIES**

Technical Information Spec-sheet

|  |
| --- |
|  SERIES NAME**URBAN** |

|  |
| --- |
| **TECHNICAL CHARACTERISTICS** |
| Available Formats: | 24x24 |
| Style Description: | Concrete | Glaze Application Method: | Inkjet |
| Visual Characteristics: | Concrete  | Number of Faces/Screens: | 8 |
| Thickness in mm: | 9,2 mm (+/-) 5% | Number of Punches/Molds: | 1 |
| Modular Suitability: | Yes | Body Type: | Porcelain |
| Application: | Residential/Commercial | Color Body Unglazed: | Off White |
| Recycled Content:Post or Pre Customer | 3% | Surface Type: | Matte/Flat/Textured |
| Rectified: | Rectified | Recommended Grout Joint: | 2 MM |

|  |
| --- |
| **PRODUCT TESTING INFORMATION** |
| *Please Note: All tests are completed per the US standards determined by the Tile Council of North America (TCNA)* |
| Water Absorption: | Eb <= 0.5% Máx. ind. 0.6% | Static COF: |  |
| Shade Variation (1, 2, 3, 4) | V3 | Dynamic COF: | Wet: 0.34; Dry: 0.64 |
| Scratch Hardness (MOHS) | 7 | Breaking Strength: | Pass |
| Frost Resistant: | Yes | Thermal Shock Resistance: |  |
| PEI/Abrasion Resistance: | 4 | Deep Abrasion Test <175mm2: | No |
| Chemical Resistance: | PASS |

*ANSI A108.02 Section 4.3.8.2 states that for running bond/joint brick patterns utilizing tiles (square or rectangle) where the side being offset is greater than 14” (nominal dimension), the running bond offset will be a maximum of 33% unless otherwise specified by the manufacturer. Use constitutes acceptance.*